Auxetic Re-entrant Honeycomb Interlayers in FDM-PETG Single-Lap Adhesive Joints: An Experimental and Machine-Learning-Guided Design

Mostofa Aadeeb Chowdhury, Sanjana Chowdhury, Md. Ashraful Islam* (corresponding author, md.islam@me.kuet.ac.bd), Md. Golam Kader.

Department of Mechanical Engineering, Khulna University of Engineering & Technology, Khulna-9203, Bangladesh.

Data Repository

This document accompanies SLJ_Auxetic_Repository.xlsx and specimens.csv, which hold the complete data and all model outputs. Failure modes were assigned per ASTM D5573 by visual inspection of the fracture surfaces.

Specimens by group

| Group | Configurations | Specimens |
| --- | --- | --- |
| Base | 1 | 4 |
| Flat | 3 | 12 |
| Spacer-2mm | 3 | 12 |
| Auxetic 45° | 9 | 36 |
| Auxetic 60° | 9 | 36 |
| Auxetic 75° | 9 | 36 |
| FGax-T1 | 3 | 12 |
| FGax-T2 | 3 | 12 |
| Validation | 4 | 16 |
| Total | 44 | 176 |

Column dictionary

| Column | Units | Description |
| --- | --- | --- |
| Specimen Id | – | Unique ID, e.g. Ax_45_1_1_S1 = auxetic, θ = 45°, t = 1 mm, IL = 1 mm, replicate 1 of 4 |
| Configuration | – | Configuration label (replicates share this; unit of the grouped cross-validation) |
| Topology type | – | Family (see table above) |
| θ | ° | Re-entrant cell angle (0 for non-auxetic families) |
| t | mm | Strut thickness (0 for solid or no-interlayer families) |
| IL | mm | Interlayer thickness (0 for Base) |
| AI | – | Auxeticity index, AI = −ν12, Masters–Evans expression under h = l |
| RD | – | Relative density of the interlayer cell |
| Porosity | % | Interlayer porosity, 100·(1 − RD) for cellular families |
| GR | – | Grading ratio (1.0 for uniform interlayers; above or below 1 only for FGax) |
| CAR | – | Cell aspect ratio (1 for every interlayer specimen, 0 for Base) |
| Epoxy | mm | Measured total epoxy thickness (training only) |
| Fmax | N | Peak tensile-shear force |
| δpeak | mm | Crosshead displacement at peak force |
| Etri | N·mm | 0.5·Fmax·δpeak, derived; triangular estimate, not an integrated energy |
| FM | – | ASTM D5573 locus-of-failure code (legend below) |

Failure-mode legend (ASTM D5573)

| Code | Meaning |
| --- | --- |
| AF | Adhesive failure (at the adherend–adhesive interface) |
| AF-M | Adhesive-mixed |
| CF | Cohesive failure (within the cured epoxy) |
| CF-M | Cohesive-mixed |
| CF-IL | Cohesive-interlayer |
| M | Mixed |
| M-B | Mixed with buckling of the interlayer strut (one validation specimen) |

Notes

Sources: Geometry, AI, RD, porosity, GR and failure-mode codes are as in Table S10 of the Supplementary Material.

Epoxy thickness: Not recorded for the validation specimens; the model inputs for the candidates assumed 0.30 mm.

Training table: The Bayesian optimizer selected the candidates with an earlier version of the training table (best configuration mean 2110.5 N); this table gives 2132.3 N. Both sets of predictions are in the workbook sheet Validation_Predictions.

Per-specimen scalar database, all 176 specimens (160 training + 16 validation)

| Specimen Id | Configuration | Topology type | θ (°) | t (mm) | IL (mm) | AI | RD | Porosity (%) | GR | CAR | Epoxy (mm) | Fmax (N) | δpeak (mm) | Etri (N·mm) | FM |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ax_45_0.8_1_S1 | Ax_45_0.8_1 | auxetic_45deg | 45 | 0.8 | 1.0 | 0.414 | 0.220 | 78.033 | 1.000 | 1 | 0.311 | 2192.02 | 1.383 | 1516.1 | CF-IL |
| Ax_45_0.8_1_S2 | Ax_45_0.8_1 | auxetic_45deg | 45 | 0.8 | 1.0 | 0.414 | 0.220 | 78.033 | 1.000 | 1 | 0.297 | 2168.01 | 1.325 | 1435.9 | CF-IL |
| Ax_45_0.8_1_S3 | Ax_45_0.8_1 | auxetic_45deg | 45 | 0.8 | 1.0 | 0.414 | 0.220 | 78.033 | 1.000 | 1 | 0.314 | 2216.03 | 1.499 | 1661.4 | CF-M |
| Ax_45_0.8_1_S4 | Ax_45_0.8_1 | auxetic_45deg | 45 | 0.8 | 1.0 | 0.414 | 0.220 | 78.033 | 1.000 | 1 | 0.334 | 1952.94 | 1.293 | 1262.5 | CF-M |
| Ax_45_1_1_S1 | Ax_45_1_1 | auxetic_45deg | 45 | 1.0 | 1.0 | 0.414 | 0.293 | 70.711 | 1.000 | 1 | 0.298 | 2034.35 | 1.225 | 1246.5 | CF-M |
| Ax_45_1_1_S2 | Ax_45_1_1 | auxetic_45deg | 45 | 1.0 | 1.0 | 0.414 | 0.293 | 70.711 | 1.000 | 1 | 0.280 | 2061.11 | 1.363 | 1404.6 | CF-M |
| Ax_45_1_1_S3 | Ax_45_1_1 | auxetic_45deg | 45 | 1.0 | 1.0 | 0.414 | 0.293 | 70.711 | 1.000 | 1 | 0.277 | 2328.67 | 1.418 | 1650.6 | M |
| Ax_45_1_1_S4 | Ax_45_1_1 | auxetic_45deg | 45 | 1.0 | 1.0 | 0.414 | 0.293 | 70.711 | 1.000 | 1 | 0.291 | 2089.75 | 1.359 | 1420.4 | M |
| Ax_45_0.6_1_S1 | Ax_45_0.6_1 | auxetic_45deg | 45 | 0.6 | 1.0 | 0.414 | 0.176 | 82.426 | 1.000 | 1 | 0.287 | 2054.65 | 1.359 | 1396.5 | CF-IL |
| Ax_45_0.6_1_S2 | Ax_45_0.6_1 | auxetic_45deg | 45 | 0.6 | 1.0 | 0.414 | 0.176 | 82.426 | 1.000 | 1 | 0.288 | 2164.28 | 1.395 | 1509.7 | CF-IL |
| Ax_45_0.6_1_S3 | Ax_45_0.6_1 | auxetic_45deg | 45 | 0.6 | 1.0 | 0.414 | 0.176 | 82.426 | 1.000 | 1 | 0.287 | 2008.72 | 1.355 | 1361.3 | CF-M |
| Ax_45_0.6_1_S4 | Ax_45_0.6_1 | auxetic_45deg | 45 | 0.6 | 1.0 | 0.414 | 0.176 | 82.426 | 1.000 | 1 | 0.280 | 2116.32 | 1.353 | 1431.8 | CF-M |
| Ax_45_0.8_0.8_S1 | Ax_45_0.8_0.8 | auxetic_45deg | 45 | 0.8 | 0.8 | 0.414 | 0.220 | 78.033 | 1.000 | 1 | 0.300 | 2148.63 | 1.302 | 1399.0 | M |
| Ax_45_0.8_0.8_S2 | Ax_45_0.8_0.8 | auxetic_45deg | 45 | 0.8 | 0.8 | 0.414 | 0.220 | 78.033 | 1.000 | 1 | 0.291 | 2070.69 | 1.289 | 1334.4 | M |
| Ax_45_0.8_0.8_S3 | Ax_45_0.8_0.8 | auxetic_45deg | 45 | 0.8 | 0.8 | 0.414 | 0.220 | 78.033 | 1.000 | 1 | 0.288 | 2031.26 | 1.254 | 1273.4 | M |
| Ax_45_0.8_0.8_S4 | Ax_45_0.8_0.8 | auxetic_45deg | 45 | 0.8 | 0.8 | 0.414 | 0.220 | 78.033 | 1.000 | 1 | 0.297 | 2016.42 | 1.230 | 1240.6 | M |
| Ax_45_1_0.8_S1 | Ax_45_1_0.8 | auxetic_45deg | 45 | 1.0 | 0.8 | 0.414 | 0.293 | 70.711 | 1.000 | 1 | 0.305 | 1982.82 | 1.202 | 1191.4 | CF-M |
| Ax_45_1_0.8_S2 | Ax_45_1_0.8 | auxetic_45deg | 45 | 1.0 | 0.8 | 0.414 | 0.293 | 70.711 | 1.000 | 1 | 0.283 | 2177.02 | 1.311 | 1427.5 | CF-M |
| Ax_45_1_0.8_S3 | Ax_45_1_0.8 | auxetic_45deg | 45 | 1.0 | 0.8 | 0.414 | 0.293 | 70.711 | 1.000 | 1 | 0.303 | 1972.41 | 1.296 | 1277.9 | M |
| Ax_45_1_0.8_S4 | Ax_45_1_0.8 | auxetic_45deg | 45 | 1.0 | 0.8 | 0.414 | 0.293 | 70.711 | 1.000 | 1 | 0.299 | 2114.95 | 1.269 | 1341.6 | M |
| Ax_45_0.6_0.8_S1 | Ax_45_0.6_0.8 | auxetic_45deg | 45 | 0.6 | 0.8 | 0.414 | 0.176 | 82.426 | 1.000 | 1 | 0.275 | 2078.67 | 1.244 | 1293.4 | CF-M |
| Ax_45_0.6_0.8_S2 | Ax_45_0.6_0.8 | auxetic_45deg | 45 | 0.6 | 0.8 | 0.414 | 0.176 | 82.426 | 1.000 | 1 | 0.308 | 1858.66 | 1.211 | 1125.4 | CF-M |
| Ax_45_0.6_0.8_S3 | Ax_45_0.6_0.8 | auxetic_45deg | 45 | 0.6 | 0.8 | 0.414 | 0.176 | 82.426 | 1.000 | 1 | 0.287 | 2034.67 | 1.268 | 1289.9 | M |
| Ax_45_0.6_0.8_S4 | Ax_45_0.6_0.8 | auxetic_45deg | 45 | 0.6 | 0.8 | 0.414 | 0.176 | 82.426 | 1.000 | 1 | 0.294 | 2109.53 | 1.410 | 1487.0 | M |
| Ax_45_1_0.6_S1 | Ax_45_1_0.6 | auxetic_45deg | 45 | 1.0 | 0.6 | 0.414 | 0.293 | 70.711 | 1.000 | 1 | 0.300 | 1929.12 | 1.072 | 1033.7 | M |
| Ax_45_1_0.6_S2 | Ax_45_1_0.6 | auxetic_45deg | 45 | 1.0 | 0.6 | 0.414 | 0.293 | 70.711 | 1.000 | 1 | 0.277 | 2172.42 | 1.231 | 1336.9 | M |
| Ax_45_1_0.6_S3 | Ax_45_1_0.6 | auxetic_45deg | 45 | 1.0 | 0.6 | 0.414 | 0.293 | 70.711 | 1.000 | 1 | 0.318 | 1896.68 | 1.107 | 1049.5 | M |
| Ax_45_1_0.6_S4 | Ax_45_1_0.6 | auxetic_45deg | 45 | 1.0 | 0.6 | 0.414 | 0.293 | 70.711 | 1.000 | 1 | 0.273 | 1977.82 | 1.193 | 1179.9 | M |
| Ax_45_0.8_0.6_S1 | Ax_45_0.8_0.6 | auxetic_45deg | 45 | 0.8 | 0.6 | 0.414 | 0.220 | 78.033 | 1.000 | 1 | 0.305 | 2029.39 | 1.176 | 1193.6 | M |
| Ax_45_0.8_0.6_S2 | Ax_45_0.8_0.6 | auxetic_45deg | 45 | 0.8 | 0.6 | 0.414 | 0.220 | 78.033 | 1.000 | 1 | 0.269 | 2026.69 | 1.194 | 1209.5 | M |
| Ax_45_0.8_0.6_S3 | Ax_45_0.8_0.6 | auxetic_45deg | 45 | 0.8 | 0.6 | 0.414 | 0.220 | 78.033 | 1.000 | 1 | 0.252 | 1935.95 | 1.207 | 1168.3 | M |
| Ax_45_0.8_0.6_S4 | Ax_45_0.8_0.6 | auxetic_45deg | 45 | 0.8 | 0.6 | 0.414 | 0.220 | 78.033 | 1.000 | 1 | 0.277 | 1880.72 | 1.148 | 1079.9 | M |
| Ax_45_0.6_0.6_S1 | Ax_45_0.6_0.6 | auxetic_45deg | 45 | 0.6 | 0.6 | 0.414 | 0.176 | 82.426 | 1.000 | 1 | 0.278 | 2041.91 | 1.278 | 1304.6 | M |
| Ax_45_0.6_0.6_S2 | Ax_45_0.6_0.6 | auxetic_45deg | 45 | 0.6 | 0.6 | 0.414 | 0.176 | 82.426 | 1.000 | 1 | 0.265 | 1724.77 | 1.083 | 933.6 | M |
| Ax_45_0.6_0.6_S3 | Ax_45_0.6_0.6 | auxetic_45deg | 45 | 0.6 | 0.6 | 0.414 | 0.176 | 82.426 | 1.000 | 1 | 0.317 | 2013.08 | 1.237 | 1245.5 | M |
| Ax_45_0.6_0.6_S4 | Ax_45_0.6_0.6 | auxetic_45deg | 45 | 0.6 | 0.6 | 0.414 | 0.176 | 82.426 | 1.000 | 1 | 0.288 | 1984.13 | 1.133 | 1123.5 | M |
| Ax_60_1_1_S1 | Ax_60_1_1 | auxetic_60deg | 60 | 1.0 | 1.0 | 0.155 | 0.366 | 63.398 | 1.000 | 1 | 0.267 | 1797.84 | 1.167 | 1048.6 | AF-M |
| Ax_60_1_1_S2 | Ax_60_1_1 | auxetic_60deg | 60 | 1.0 | 1.0 | 0.155 | 0.366 | 63.398 | 1.000 | 1 | 0.316 | 2026.80 | 1.166 | 1182.1 | CF-M |
| Ax_60_1_1_S3 | Ax_60_1_1 | auxetic_60deg | 60 | 1.0 | 1.0 | 0.155 | 0.366 | 63.398 | 1.000 | 1 | 0.288 | 1772.40 | 1.147 | 1016.7 | CF-M |
| Ax_60_1_1_S4 | Ax_60_1_1 | auxetic_60deg | 60 | 1.0 | 1.0 | 0.155 | 0.366 | 63.398 | 1.000 | 1 | 0.289 | 1749.77 | 1.017 | 889.3 | M |
| Ax_60_0.8_1_S1 | Ax_60_0.8_1 | auxetic_60deg | 60 | 0.8 | 1.0 | 0.155 | 0.275 | 72.548 | 1.000 | 1 | 0.285 | 1901.98 | 1.223 | 1163.4 | AF-M |
| Ax_60_0.8_1_S2 | Ax_60_0.8_1 | auxetic_60deg | 60 | 0.8 | 1.0 | 0.155 | 0.275 | 72.548 | 1.000 | 1 | 0.313 | 1742.02 | 1.104 | 962.0 | CF-M |
| Ax_60_0.8_1_S3 | Ax_60_0.8_1 | auxetic_60deg | 60 | 0.8 | 1.0 | 0.155 | 0.275 | 72.548 | 1.000 | 1 | 0.323 | 1885.98 | 1.147 | 1081.5 | CF-M |
| Ax_60_0.8_1_S4 | Ax_60_0.8_1 | auxetic_60deg | 60 | 0.8 | 1.0 | 0.155 | 0.275 | 72.548 | 1.000 | 1 | 0.320 | 1757.97 | 1.114 | 979.2 | M |
| Ax_60_0.6_1_S1 | Ax_60_0.6_1 | auxetic_60deg | 60 | 0.6 | 1.0 | 0.155 | 0.220 | 78.038 | 1.000 | 1 | 0.305 | 1681.41 | 1.098 | 923.2 | AF-M |
| Ax_60_0.6_1_S2 | Ax_60_0.6_1 | auxetic_60deg | 60 | 0.6 | 1.0 | 0.155 | 0.220 | 78.038 | 1.000 | 1 | 0.313 | 1845.16 | 1.168 | 1077.9 | CF-M |
| Ax_60_0.6_1_S3 | Ax_60_0.6_1 | auxetic_60deg | 60 | 0.6 | 1.0 | 0.155 | 0.220 | 78.038 | 1.000 | 1 | 0.280 | 1768.10 | 1.123 | 993.2 | CF-M |
| Ax_60_0.6_1_S4 | Ax_60_0.6_1 | auxetic_60deg | 60 | 0.6 | 1.0 | 0.155 | 0.220 | 78.038 | 1.000 | 1 | 0.298 | 1893.72 | 1.199 | 1135.0 | M |
| Ax_60_1_0.8_S1 | Ax_60_1_0.8 | auxetic_60deg | 60 | 1.0 | 0.8 | 0.155 | 0.366 | 63.398 | 1.000 | 1 | 0.326 | 1729.93 | 1.071 | 926.2 | AF-M |
| Ax_60_1_0.8_S2 | Ax_60_1_0.8 | auxetic_60deg | 60 | 1.0 | 0.8 | 0.155 | 0.366 | 63.398 | 1.000 | 1 | 0.280 | 1676.87 | 0.947 | 794.2 | M |
| Ax_60_1_0.8_S3 | Ax_60_1_0.8 | auxetic_60deg | 60 | 1.0 | 0.8 | 0.155 | 0.366 | 63.398 | 1.000 | 1 | 0.318 | 1910.36 | 1.101 | 1051.3 | M |
| Ax_60_1_0.8_S4 | Ax_60_1_0.8 | auxetic_60deg | 60 | 1.0 | 0.8 | 0.155 | 0.366 | 63.398 | 1.000 | 1 | 0.309 | 1815.43 | 1.056 | 958.7 | M |
| Ax_60_0.8_0.8_S1 | Ax_60_0.8_0.8 | auxetic_60deg | 60 | 0.8 | 0.8 | 0.155 | 0.275 | 72.548 | 1.000 | 1 | 0.279 | 1856.80 | 1.134 | 1052.6 | AF-M |
| Ax_60_0.8_0.8_S2 | Ax_60_0.8_0.8 | auxetic_60deg | 60 | 0.8 | 0.8 | 0.155 | 0.275 | 72.548 | 1.000 | 1 | 0.317 | 1827.53 | 1.041 | 951.5 | M |
| Ax_60_0.8_0.8_S3 | Ax_60_0.8_0.8 | auxetic_60deg | 60 | 0.8 | 0.8 | 0.155 | 0.275 | 72.548 | 1.000 | 1 | 0.286 | 1608.03 | 1.025 | 824.3 | M |
| Ax_60_0.8_0.8_S4 | Ax_60_0.8_0.8 | auxetic_60deg | 60 | 0.8 | 0.8 | 0.155 | 0.275 | 72.548 | 1.000 | 1 | 0.315 | 1784.53 | 1.026 | 915.4 | M |
| Ax_60_0.6_0.8_S1 | Ax_60_0.6_0.8 | auxetic_60deg | 60 | 0.6 | 0.8 | 0.155 | 0.220 | 78.038 | 1.000 | 1 | 0.302 | 1649.61 | 1.019 | 840.1 | AF-M |
| Ax_60_0.6_0.8_S2 | Ax_60_0.6_0.8 | auxetic_60deg | 60 | 0.6 | 0.8 | 0.155 | 0.220 | 78.038 | 1.000 | 1 | 0.293 | 1917.05 | 1.112 | 1066.3 | AF-M |
| Ax_60_0.6_0.8_S3 | Ax_60_0.6_0.8 | auxetic_60deg | 60 | 0.6 | 0.8 | 0.155 | 0.220 | 78.038 | 1.000 | 1 | 0.302 | 1681.07 | 1.037 | 871.6 | M |
| Ax_60_0.6_0.8_S4 | Ax_60_0.6_0.8 | auxetic_60deg | 60 | 0.6 | 0.8 | 0.155 | 0.220 | 78.038 | 1.000 | 1 | 0.256 | 1728.77 | 1.099 | 949.6 | M |
| Ax_60_1_0.6_S1 | Ax_60_1_0.6 | auxetic_60deg | 60 | 1.0 | 0.6 | 0.155 | 0.366 | 63.398 | 1.000 | 1 | 0.319 | 1603.18 | 0.905 | 725.8 | AF-M |
| Ax_60_1_0.6_S2 | Ax_60_1_0.6 | auxetic_60deg | 60 | 1.0 | 0.6 | 0.155 | 0.366 | 63.398 | 1.000 | 1 | 0.350 | 1745.12 | 0.984 | 858.8 | AF-M |
| Ax_60_1_0.6_S3 | Ax_60_1_0.6 | auxetic_60deg | 60 | 1.0 | 0.6 | 0.155 | 0.366 | 63.398 | 1.000 | 1 | 0.336 | 1784.92 | 1.018 | 908.7 | M |
| Ax_60_1_0.6_S4 | Ax_60_1_0.6 | auxetic_60deg | 60 | 1.0 | 0.6 | 0.155 | 0.366 | 63.398 | 1.000 | 1 | 0.318 | 1783.78 | 0.968 | 863.5 | M |
| Ax_60_0.8_0.6_S1 | Ax_60_0.8_0.6 | auxetic_60deg | 60 | 0.8 | 0.6 | 0.155 | 0.275 | 72.548 | 1.000 | 1 | 0.311 | 1740.44 | 0.955 | 831.2 | AF |
| Ax_60_0.8_0.6_S2 | Ax_60_0.8_0.6 | auxetic_60deg | 60 | 0.8 | 0.6 | 0.155 | 0.275 | 72.548 | 1.000 | 1 | 0.325 | 1757.40 | 1.004 | 882.0 | M |
| Ax_60_0.8_0.6_S3 | Ax_60_0.8_0.6 | auxetic_60deg | 60 | 0.8 | 0.6 | 0.155 | 0.275 | 72.548 | 1.000 | 1 | 0.306 | 1587.80 | 0.936 | 742.8 | M |
| Ax_60_0.8_0.6_S4 | Ax_60_0.8_0.6 | auxetic_60deg | 60 | 0.8 | 0.6 | 0.155 | 0.275 | 72.548 | 1.000 | 1 | 0.311 | 1774.39 | 1.050 | 931.3 | M |
| Ax_60_0.6_0.6_S1 | Ax_60_0.6_0.6 | auxetic_60deg | 60 | 0.6 | 0.6 | 0.155 | 0.220 | 78.038 | 1.000 | 1 | 0.330 | 1662.08 | 1.008 | 837.4 | AF |
| Ax_60_0.6_0.6_S2 | Ax_60_0.6_0.6 | auxetic_60deg | 60 | 0.6 | 0.6 | 0.155 | 0.220 | 78.038 | 1.000 | 1 | 0.304 | 1829.60 | 1.024 | 936.5 | AF-M |
| Ax_60_0.6_0.6_S3 | Ax_60_0.6_0.6 | auxetic_60deg | 60 | 0.6 | 0.6 | 0.155 | 0.220 | 78.038 | 1.000 | 1 | 0.293 | 1643.47 | 0.998 | 820.4 | M |
| Ax_60_0.6_0.6_S4 | Ax_60_0.6_0.6 | auxetic_60deg | 60 | 0.6 | 0.6 | 0.155 | 0.220 | 78.038 | 1.000 | 1 | 0.315 | 1624.60 | 0.915 | 743.4 | M |
| Ax_75_1_1_S1 | Ax_75_1_1 | auxetic_75deg | 75 | 1.0 | 1.0 | 0.035 | 0.659 | 34.108 | 1.000 | 1 | 0.270 | 1562.40 | 1.029 | 803.8 | AF-M |
| Ax_75_1_1_S2 | Ax_75_1_1 | auxetic_75deg | 75 | 1.0 | 1.0 | 0.035 | 0.659 | 34.108 | 1.000 | 1 | 0.278 | 1663.60 | 1.038 | 863.0 | AF-M |
| Ax_75_1_1_S3 | Ax_75_1_1 | auxetic_75deg | 75 | 1.0 | 1.0 | 0.035 | 0.659 | 34.108 | 1.000 | 1 | 0.303 | 1676.25 | 1.078 | 903.9 | CF |
| Ax_75_1_1_S4 | Ax_75_1_1 | auxetic_75deg | 75 | 1.0 | 1.0 | 0.035 | 0.659 | 34.108 | 1.000 | 1 | 0.273 | 1550.85 | 1.004 | 778.4 | CF |
| Ax_75_0.8_1_S1 | Ax_75_0.8_1 | auxetic_75deg | 75 | 0.8 | 1.0 | 0.035 | 0.494 | 50.581 | 1.000 | 1 | 0.292 | 1576.68 | 1.020 | 804.0 | AF-M |
| Ax_75_0.8_1_S2 | Ax_75_0.8_1 | auxetic_75deg | 75 | 0.8 | 1.0 | 0.035 | 0.494 | 50.581 | 1.000 | 1 | 0.282 | 1673.42 | 1.090 | 912.2 | AF-M |
| Ax_75_0.8_1_S3 | Ax_75_0.8_1 | auxetic_75deg | 75 | 0.8 | 1.0 | 0.035 | 0.494 | 50.581 | 1.000 | 1 | 0.296 | 1636.21 | 1.051 | 859.9 | CF |
| Ax_75_0.8_1_S4 | Ax_75_0.8_1 | auxetic_75deg | 75 | 0.8 | 1.0 | 0.035 | 0.494 | 50.581 | 1.000 | 1 | 0.309 | 1510.14 | 1.012 | 763.9 | CF |
| Ax_75_0.6_1_S1 | Ax_75_0.6_1 | auxetic_75deg | 75 | 0.6 | 1.0 | 0.035 | 0.395 | 60.465 | 1.000 | 1 | 0.306 | 1605.96 | 1.074 | 862.4 | AF |
| Ax_75_0.6_1_S2 | Ax_75_0.6_1 | auxetic_75deg | 75 | 0.6 | 1.0 | 0.035 | 0.395 | 60.465 | 1.000 | 1 | 0.298 | 1542.07 | 1.062 | 819.2 | AF-M |
| Ax_75_0.6_1_S3 | Ax_75_0.6_1 | auxetic_75deg | 75 | 0.6 | 1.0 | 0.035 | 0.395 | 60.465 | 1.000 | 1 | 0.258 | 1512.13 | 0.991 | 749.4 | CF |
| Ax_75_0.6_1_S4 | Ax_75_0.6_1 | auxetic_75deg | 75 | 0.6 | 1.0 | 0.035 | 0.395 | 60.465 | 1.000 | 1 | 0.299 | 1670.89 | 1.086 | 907.6 | CF |
| FGax_T1_1mm_S1 | FGax_T1_1mm | fgax_t1 | 45 | 1.0 | 1.0 | 0.225 | 0.320 | 67.968 | 11.742 | 1 | 0.301 | 1579.09 | 0.965 | 761.9 | CF-M |
| FGax_T1_1mm_S2 | FGax_T1_1mm | fgax_t1 | 45 | 1.0 | 1.0 | 0.225 | 0.320 | 67.968 | 11.742 | 1 | 0.350 | 1697.25 | 1.040 | 882.9 | CF-IL |
| FGax_T1_1mm_S3 | FGax_T1_1mm | fgax_t1 | 45 | 1.0 | 1.0 | 0.225 | 0.320 | 67.968 | 11.742 | 1 | 0.296 | 1662.04 | 0.986 | 819.5 | CF-IL |
| FGax_T1_1mm_S4 | FGax_T1_1mm | fgax_t1 | 45 | 1.0 | 1.0 | 0.225 | 0.320 | 67.968 | 11.742 | 1 | 0.307 | 1683.16 | 1.000 | 841.5 | CF-IL |
| Ax_75_1_0.8_S1 | Ax_75_1_0.8 | auxetic_75deg | 75 | 1.0 | 0.8 | 0.035 | 0.659 | 34.108 | 1.000 | 1 | 0.343 | 1545.05 | 0.962 | 743.4 | AF |
| Ax_75_1_0.8_S2 | Ax_75_1_0.8 | auxetic_75deg | 75 | 1.0 | 0.8 | 0.035 | 0.659 | 34.108 | 1.000 | 1 | 0.257 | 1667.36 | 1.030 | 858.7 | AF-M |
| Ax_75_1_0.8_S3 | Ax_75_1_0.8 | auxetic_75deg | 75 | 1.0 | 0.8 | 0.035 | 0.659 | 34.108 | 1.000 | 1 | 0.283 | 1557.51 | 1.019 | 793.9 | AF-M |
| Ax_75_1_0.8_S4 | Ax_75_1_0.8 | auxetic_75deg | 75 | 1.0 | 0.8 | 0.035 | 0.659 | 34.108 | 1.000 | 1 | 0.304 | 1530.08 | 0.938 | 717.5 | CF |
| FGax_T1_0.8mm_S1 | FGax_T1_0.8mm | fgax_t1 | 45 | 1.0 | 0.8 | 0.225 | 0.320 | 67.968 | 11.742 | 1 | 0.282 | 1605.99 | 0.944 | 758.3 | M |
| FGax_T1_0.8mm_S2 | FGax_T1_0.8mm | fgax_t1 | 45 | 1.0 | 0.8 | 0.225 | 0.320 | 67.968 | 11.742 | 1 | 0.330 | 1594.48 | 0.924 | 736.9 | CF-M |
| FGax_T1_0.8mm_S3 | FGax_T1_0.8mm | fgax_t1 | 45 | 1.0 | 0.8 | 0.225 | 0.320 | 67.968 | 11.742 | 1 | 0.331 | 1717.94 | 1.007 | 864.8 | CF-IL |
| FGax_T1_0.8mm_S4 | FGax_T1_0.8mm | fgax_t1 | 45 | 1.0 | 0.8 | 0.225 | 0.320 | 67.968 | 11.742 | 1 | 0.331 | 1677.67 | 0.997 | 836.0 | CF-IL |
| FGax_T1_0.6mm_S1 | FGax_T1_0.6mm | fgax_t1 | 45 | 1.0 | 0.6 | 0.225 | 0.320 | 67.968 | 11.742 | 1 | 0.279 | 1672.72 | 0.961 | 804.1 | M |
| FGax_T1_0.6mm_S2 | FGax_T1_0.6mm | fgax_t1 | 45 | 1.0 | 0.6 | 0.225 | 0.320 | 67.968 | 11.742 | 1 | 0.328 | 1678.51 | 0.947 | 794.7 | CF-M |
| FGax_T1_0.6mm_S3 | FGax_T1_0.6mm | fgax_t1 | 45 | 1.0 | 0.6 | 0.225 | 0.320 | 67.968 | 11.742 | 1 | 0.302 | 1558.94 | 0.910 | 709.3 | CF-M |
| FGax_T1_0.6mm_S4 | FGax_T1_0.6mm | fgax_t1 | 45 | 1.0 | 0.6 | 0.225 | 0.320 | 67.968 | 11.742 | 1 | 0.313 | 1664.31 | 0.933 | 776.1 | CF-IL |
| Base_S1 | Base | base | 0 | 0.0 | 0.0 | 0.000 | 1.000 | 0.000 | 1.000 | 0 | 0.300 | 1613.07 | 1.013 | 817.2 | AF |
| Base_S2 | Base | base | 0 | 0.0 | 0.0 | 0.000 | 1.000 | 0.000 | 1.000 | 0 | 0.292 | 1641.50 | 0.993 | 814.6 | CF |
| Base_S3 | Base | base | 0 | 0.0 | 0.0 | 0.000 | 1.000 | 0.000 | 1.000 | 0 | 0.314 | 1624.64 | 1.035 | 840.7 | CF |
| Base_S4 | Base | base | 0 | 0.0 | 0.0 | 0.000 | 1.000 | 0.000 | 1.000 | 0 | 0.273 | 1688.30 | 1.043 | 880.1 | CF |
| Ax_75_0.8_0.8_S1 | Ax_75_0.8_0.8 | auxetic_75deg | 75 | 0.8 | 0.8 | 0.035 | 0.494 | 50.581 | 1.000 | 1 | 0.309 | 1605.82 | 1.052 | 844.3 | AF |
| Ax_75_0.8_0.8_S2 | Ax_75_0.8_0.8 | auxetic_75deg | 75 | 0.8 | 0.8 | 0.035 | 0.494 | 50.581 | 1.000 | 1 | 0.250 | 1521.55 | 0.972 | 739.8 | AF-M |
| Ax_75_0.8_0.8_S3 | Ax_75_0.8_0.8 | auxetic_75deg | 75 | 0.8 | 0.8 | 0.035 | 0.494 | 50.581 | 1.000 | 1 | 0.311 | 1596.45 | 0.979 | 781.8 | AF-M |
| Ax_75_0.8_0.8_S4 | Ax_75_0.8_0.8 | auxetic_75deg | 75 | 0.8 | 0.8 | 0.035 | 0.494 | 50.581 | 1.000 | 1 | 0.320 | 1514.23 | 0.971 | 735.4 | AF-M |
| FGax_T2_1mm_S1 | FGax_T2_1mm | fgax_t2 | 75 | 0.8 | 1.0 | 0.225 | 0.320 | 67.968 | 0.085 | 1 | 0.318 | 1589.73 | 1.069 | 849.5 | M |
| FGax_T2_1mm_S2 | FGax_T2_1mm | fgax_t2 | 75 | 0.8 | 1.0 | 0.225 | 0.320 | 67.968 | 0.085 | 1 | 0.273 | 1658.57 | 1.134 | 940.5 | CF-M |
| FGax_T2_1mm_S3 | FGax_T2_1mm | fgax_t2 | 75 | 0.8 | 1.0 | 0.225 | 0.320 | 67.968 | 0.085 | 1 | 0.305 | 1658.78 | 1.119 | 927.8 | CF-IL |
| FGax_T2_1mm_S4 | FGax_T2_1mm | fgax_t2 | 75 | 0.8 | 1.0 | 0.225 | 0.320 | 67.968 | 0.085 | 1 | 0.329 | 1611.13 | 1.076 | 866.9 | CF-IL |
| Ax_75_0.6_0.8_S1 | Ax_75_0.6_0.8 | auxetic_75deg | 75 | 0.6 | 0.8 | 0.035 | 0.395 | 60.465 | 1.000 | 1 | 0.322 | 1619.06 | 1.026 | 830.8 | AF |
| Ax_75_0.6_0.8_S2 | Ax_75_0.6_0.8 | auxetic_75deg | 75 | 0.6 | 0.8 | 0.035 | 0.395 | 60.465 | 1.000 | 1 | 0.303 | 1485.34 | 0.960 | 713.1 | AF |
| Ax_75_0.6_0.8_S3 | Ax_75_0.6_0.8 | auxetic_75deg | 75 | 0.6 | 0.8 | 0.035 | 0.395 | 60.465 | 1.000 | 1 | 0.287 | 1562.77 | 1.008 | 787.8 | AF-M |
| Ax_75_0.6_0.8_S4 | Ax_75_0.6_0.8 | auxetic_75deg | 75 | 0.6 | 0.8 | 0.035 | 0.395 | 60.465 | 1.000 | 1 | 0.278 | 1512.72 | 1.020 | 771.5 | AF-M |
| FGax_T2_0.8mm_S1 | FGax_T2_0.8mm | fgax_t2 | 75 | 0.8 | 0.8 | 0.225 | 0.320 | 67.968 | 0.085 | 1 | 0.306 | 1667.73 | 1.139 | 949.7 | M |
| FGax_T2_0.8mm_S2 | FGax_T2_0.8mm | fgax_t2 | 75 | 0.8 | 0.8 | 0.225 | 0.320 | 67.968 | 0.085 | 1 | 0.308 | 1632.12 | 1.040 | 848.5 | M |
| FGax_T2_0.8mm_S3 | FGax_T2_0.8mm | fgax_t2 | 75 | 0.8 | 0.8 | 0.225 | 0.320 | 67.968 | 0.085 | 1 | 0.285 | 1532.40 | 1.043 | 798.8 | CF-M |
| FGax_T2_0.8mm_S4 | FGax_T2_0.8mm | fgax_t2 | 75 | 0.8 | 0.8 | 0.225 | 0.320 | 67.968 | 0.085 | 1 | 0.305 | 1659.48 | 1.057 | 877.3 | CF-M |
| FGax_T2_0.6mm_S1 | FGax_T2_0.6mm | fgax_t2 | 75 | 0.8 | 0.6 | 0.225 | 0.320 | 67.968 | 0.085 | 1 | 0.306 | 1727.66 | 1.090 | 941.8 | M |
| FGax_T2_0.6mm_S2 | FGax_T2_0.6mm | fgax_t2 | 75 | 0.8 | 0.6 | 0.225 | 0.320 | 67.968 | 0.085 | 1 | 0.284 | 1557.63 | 1.006 | 783.2 | M |
| FGax_T2_0.6mm_S3 | FGax_T2_0.6mm | fgax_t2 | 75 | 0.8 | 0.6 | 0.225 | 0.320 | 67.968 | 0.085 | 1 | 0.341 | 1607.11 | 1.081 | 868.8 | M |
| FGax_T2_0.6mm_S4 | FGax_T2_0.6mm | fgax_t2 | 75 | 0.8 | 0.6 | 0.225 | 0.320 | 67.968 | 0.085 | 1 | 0.310 | 1577.42 | 1.022 | 805.7 | CF-M |
| Ax_75_1_0.6_S1 | Ax_75_1_0.6 | auxetic_75deg | 75 | 1.0 | 0.6 | 0.035 | 0.659 | 34.108 | 1.000 | 1 | 0.271 | 1506.53 | 0.934 | 703.7 | AF |
| Ax_75_1_0.6_S2 | Ax_75_1_0.6 | auxetic_75deg | 75 | 1.0 | 0.6 | 0.035 | 0.659 | 34.108 | 1.000 | 1 | 0.299 | 1582.86 | 0.971 | 768.5 | AF-M |
| Ax_75_1_0.6_S3 | Ax_75_1_0.6 | auxetic_75deg | 75 | 1.0 | 0.6 | 0.035 | 0.659 | 34.108 | 1.000 | 1 | 0.330 | 1502.33 | 0.903 | 678.1 | AF-M |
| Ax_75_1_0.6_S4 | Ax_75_1_0.6 | auxetic_75deg | 75 | 1.0 | 0.6 | 0.035 | 0.659 | 34.108 | 1.000 | 1 | 0.284 | 1557.31 | 0.942 | 733.1 | CF |
| Ax_75_0.8_0.6_S1 | Ax_75_0.8_0.6 | auxetic_75deg | 75 | 0.8 | 0.6 | 0.035 | 0.494 | 50.581 | 1.000 | 1 | 0.268 | 1452.56 | 0.921 | 669.2 | AF |
| Ax_75_0.8_0.6_S2 | Ax_75_0.8_0.6 | auxetic_75deg | 75 | 0.8 | 0.6 | 0.035 | 0.494 | 50.581 | 1.000 | 1 | 0.303 | 1553.98 | 0.973 | 755.9 | AF |
| Ax_75_0.8_0.6_S3 | Ax_75_0.8_0.6 | auxetic_75deg | 75 | 0.8 | 0.6 | 0.035 | 0.494 | 50.581 | 1.000 | 1 | 0.270 | 1548.70 | 0.943 | 730.0 | AF-M |
| Ax_75_0.8_0.6_S4 | Ax_75_0.8_0.6 | auxetic_75deg | 75 | 0.8 | 0.6 | 0.035 | 0.494 | 50.581 | 1.000 | 1 | 0.283 | 1538.42 | 0.939 | 722.1 | AF-M |
| Ax_75_0.6_0.6_S1 | Ax_75_0.6_0.6 | auxetic_75deg | 75 | 0.6 | 0.6 | 0.035 | 0.395 | 60.465 | 1.000 | 1 | 0.300 | 1482.67 | 0.961 | 712.7 | AF |
| Ax_75_0.6_0.6_S2 | Ax_75_0.6_0.6 | auxetic_75deg | 75 | 0.6 | 0.6 | 0.035 | 0.395 | 60.465 | 1.000 | 1 | 0.309 | 1511.63 | 0.901 | 680.8 | AF |
| Ax_75_0.6_0.6_S3 | Ax_75_0.6_0.6 | auxetic_75deg | 75 | 0.6 | 0.6 | 0.035 | 0.395 | 60.465 | 1.000 | 1 | 0.297 | 1596.00 | 0.973 | 776.6 | AF-M |
| Ax_75_0.6_0.6_S4 | Ax_75_0.6_0.6 | auxetic_75deg | 75 | 0.6 | 0.6 | 0.035 | 0.395 | 60.465 | 1.000 | 1 | 0.319 | 1494.00 | 0.980 | 732.4 | AF-M |
| Flat_1mm_S1 | Flat_1mm | flat | 0 | 0.0 | 1.0 | 0.000 | 1.000 | 0.000 | 1.000 | 1 | 0.294 | 1491.35 | 0.995 | 741.9 | CF |
| Flat_1mm_S2 | Flat_1mm | flat | 0 | 0.0 | 1.0 | 0.000 | 1.000 | 0.000 | 1.000 | 1 | 0.350 | 1483.10 | 1.020 | 756.2 | CF |
| Flat_1mm_S3 | Flat_1mm | flat | 0 | 0.0 | 1.0 | 0.000 | 1.000 | 0.000 | 1.000 | 1 | 0.314 | 1573.81 | 1.054 | 829.5 | CF |
| Flat_1mm_S4 | Flat_1mm | flat | 0 | 0.0 | 1.0 | 0.000 | 1.000 | 0.000 | 1.000 | 1 | 0.281 | 1564.65 | 1.026 | 802.5 | CF |
| Flat_0.8mm_S1 | Flat_0.8mm | flat | 0 | 0.0 | 0.8 | 0.000 | 1.000 | 0.000 | 1.000 | 1 | 0.276 | 1447.70 | 1.003 | 725.8 | AF-M |
| Flat_0.8mm_S2 | Flat_0.8mm | flat | 0 | 0.0 | 0.8 | 0.000 | 1.000 | 0.000 | 1.000 | 1 | 0.311 | 1565.72 | 1.030 | 806.3 | CF |
| Flat_0.8mm_S3 | Flat_0.8mm | flat | 0 | 0.0 | 0.8 | 0.000 | 1.000 | 0.000 | 1.000 | 1 | 0.295 | 1538.86 | 1.012 | 778.5 | CF |
| Flat_0.8mm_S4 | Flat_0.8mm | flat | 0 | 0.0 | 0.8 | 0.000 | 1.000 | 0.000 | 1.000 | 1 | 0.316 | 1495.88 | 0.965 | 721.8 | CF |
| Flat_0.6mm_S1 | Flat_0.6mm | flat | 0 | 0.0 | 0.6 | 0.000 | 1.000 | 0.000 | 1.000 | 1 | 0.313 | 1466.23 | 0.993 | 728.3 | AF |
| Flat_0.6mm_S2 | Flat_0.6mm | flat | 0 | 0.0 | 0.6 | 0.000 | 1.000 | 0.000 | 1.000 | 1 | 0.257 | 1564.05 | 1.022 | 799.3 | AF-M |
| Flat_0.6mm_S3 | Flat_0.6mm | flat | 0 | 0.0 | 0.6 | 0.000 | 1.000 | 0.000 | 1.000 | 1 | 0.307 | 1438.66 | 0.974 | 700.9 | CF |
| Flat_0.6mm_S4 | Flat_0.6mm | flat | 0 | 0.0 | 0.6 | 0.000 | 1.000 | 0.000 | 1.000 | 1 | 0.301 | 1512.26 | 1.042 | 787.9 | CF |
| Spacer_2mm_1mm_S1 | Spacer_2mm_1mm | spacer_2mm | 0 | 2.0 | 1.0 | 0.000 | 0.804 | 19.635 | 1.000 | 1 | 0.323 | 1447.95 | 0.952 | 689.4 | CF |
| Spacer_2mm_1mm_S2 | Spacer_2mm_1mm | spacer_2mm | 0 | 2.0 | 1.0 | 0.000 | 0.804 | 19.635 | 1.000 | 1 | 0.292 | 1531.34 | 1.069 | 818.2 | CF |
| Spacer_2mm_1mm_S3 | Spacer_2mm_1mm | spacer_2mm | 0 | 2.0 | 1.0 | 0.000 | 0.804 | 19.635 | 1.000 | 1 | 0.280 | 1536.56 | 1.005 | 771.8 | CF |
| Spacer_2mm_1mm_S4 | Spacer_2mm_1mm | spacer_2mm | 0 | 2.0 | 1.0 | 0.000 | 0.804 | 19.635 | 1.000 | 1 | 0.289 | 1514.39 | 1.038 | 786.0 | CF |
| Spacer_2mm_0.8mm_S1 | Spacer_2mm_0.8mm | spacer_2mm | 0 | 2.0 | 0.8 | 0.000 | 0.804 | 19.635 | 1.000 | 1 | 0.295 | 1426.46 | 0.929 | 662.4 | AF |
| Spacer_2mm_0.8mm_S2 | Spacer_2mm_0.8mm | spacer_2mm | 0 | 2.0 | 0.8 | 0.000 | 0.804 | 19.635 | 1.000 | 1 | 0.271 | 1562.62 | 1.022 | 798.4 | CF |
| Spacer_2mm_0.8mm_S3 | Spacer_2mm_0.8mm | spacer_2mm | 0 | 2.0 | 0.8 | 0.000 | 0.804 | 19.635 | 1.000 | 1 | 0.323 | 1441.77 | 0.971 | 699.8 | CF |
| Spacer_2mm_0.8mm_S4 | Spacer_2mm_0.8mm | spacer_2mm | 0 | 2.0 | 0.8 | 0.000 | 0.804 | 19.635 | 1.000 | 1 | 0.313 | 1465.94 | 1.065 | 780.5 | CF |
| Spacer_2mm_0.6mm_S1 | Spacer_2mm_0.6mm | spacer_2mm | 0 | 2.0 | 0.6 | 0.000 | 0.804 | 19.635 | 1.000 | 1 | 0.301 | 1522.58 | 0.948 | 721.5 | AF |
| Spacer_2mm_0.6mm_S2 | Spacer_2mm_0.6mm | spacer_2mm | 0 | 2.0 | 0.6 | 0.000 | 0.804 | 19.635 | 1.000 | 1 | 0.291 | 1386.28 | 0.968 | 671.2 | CF |
| Spacer_2mm_0.6mm_S3 | Spacer_2mm_0.6mm | spacer_2mm | 0 | 2.0 | 0.6 | 0.000 | 0.804 | 19.635 | 1.000 | 1 | 0.342 | 1371.14 | 0.961 | 659.0 | CF |
| Spacer_2mm_0.6mm_S4 | Spacer_2mm_0.6mm | spacer_2mm | 0 | 2.0 | 0.6 | 0.000 | 0.804 | 19.635 | 1.000 | 1 | 0.285 | 1356.00 | 0.944 | 640.1 | CF |
| V-α_1 | V-α | validation | 43 | 0.4 | 1.1 | 0.466 | 0.425 | 57.530 | 1.000 | 1 |  | 1873.50 | 1.150 | 1077.3 | AF-M |
| V-α_2 | V-α | validation | 43 | 0.4 | 1.1 | 0.466 | 0.425 | 57.530 | 1.000 | 1 |  | 2194.70 | 1.440 | 1580.2 | CF |
| V-α_3 | V-α | validation | 43 | 0.4 | 1.1 | 0.466 | 0.425 | 57.530 | 1.000 | 1 |  | 1928.10 | 1.170 | 1127.9 | CF-M |
| V-α_4 | V-α | validation | 43 | 0.4 | 1.1 | 0.466 | 0.425 | 57.530 | 1.000 | 1 |  | 2051.30 | 1.310 | 1343.6 | CF |
| V-β_1 | V-β | validation | 40 | 0.4 | 0.8 | 0.556 | 0.385 | 61.530 | 1.000 | 1 |  | 2293.60 | 1.300 | 1490.8 | CF-IL |
| V-β_2 | V-β | validation | 40 | 0.4 | 0.8 | 0.556 | 0.385 | 61.530 | 1.000 | 1 |  | 2114.80 | 1.150 | 1216.0 | M |
| V-β_3 | V-β | validation | 40 | 0.4 | 0.8 | 0.556 | 0.385 | 61.530 | 1.000 | 1 |  | 2240.20 | 1.260 | 1411.3 | CF-IL |
| V-β_4 | V-β | validation | 40 | 0.4 | 0.8 | 0.556 | 0.385 | 61.530 | 1.000 | 1 |  | 2075.90 | 1.130 | 1172.9 | CF-IL |
| V-δ_1 | V-δ | validation | 38 | 0.6 | 0.8 | 0.624 | 0.550 | 45.000 | 1.000 | 1 |  | 2094.20 | 1.060 | 1109.9 | M-B |
| V-δ_2 | V-δ | validation | 38 | 0.6 | 0.8 | 0.624 | 0.550 | 45.000 | 1.000 | 1 |  | 2388.70 | 1.330 | 1588.5 | CF-IL |
| V-δ_3 | V-δ | validation | 38 | 0.6 | 0.8 | 0.624 | 0.550 | 45.000 | 1.000 | 1 |  | 2173.50 | 1.160 | 1260.6 | CF-IL |
| V-δ_4 | V-δ | validation | 38 | 0.6 | 0.8 | 0.624 | 0.550 | 45.000 | 1.000 | 1 |  | 2266.10 | 1.250 | 1416.3 | CF-IL |
| V-ε_1 | V-ε | validation | 45 | 0.4 | 0.8 | 0.414 | 0.439 | 56.070 | 1.000 | 1 |  | 2079.40 | 1.170 | 1216.4 | CF |
| V-ε_2 | V-ε | validation | 45 | 0.4 | 0.8 | 0.414 | 0.439 | 56.070 | 1.000 | 1 |  | 1805.70 | 0.880 | 794.5 | AF-M |
| V-ε_3 | V-ε | validation | 45 | 0.4 | 0.8 | 0.414 | 0.439 | 56.070 | 1.000 | 1 |  | 1963.80 | 1.050 | 1031.0 | CF-M |
| V-ε_4 | V-ε | validation | 45 | 0.4 | 0.8 | 0.414 | 0.439 | 56.070 | 1.000 | 1 |  | 1894.60 | 0.950 | 899.9 | CF |